| Should be used |  |
| --- | --- |
|  | • Rotary screw compressors for cooling lubricants • Recommended in the outlet temperature> 90 ℃, and / or export> 10bars use |

| Characteristics |  |
| --- | --- |
|  | • You can optimize the efficiency of the compressor • Good oil / gas and oil / condensate separation performance • protection against wear or corrosion screw • compressed air can really reduce the operating costs • Use the most efficient compressor • increase oil change intervals, drain intervals may be fixed compressors generally use 4000 ~ 6000 hours • If lubrication monitoring, up to 8000 hours • You can extend the life of the separator filter unit • Excellent anti-clogging performance, using a filter with an extended period (up to 8000 hours) |

| Technical Specifications |  |
| --- | --- |
|  | Typical data; Unit; Test method; DACNIS SH. 32; 46; 68; 100. Density (15 ℃); kg/m3; ASTM D1298; 859; 862; 840; 869. Viscosity (40 ℃); mm2/s; ASTM D445; 32; 46; 68; 100. Viscosity Index; -; ASTM D2270; 136; 139; 147; 143. Pour Point ℃; ℃; ASTM D97; <-42; <-42; <-42; <-39. Flash point (open cup); ℃; ASTM D92; 250; 255; 262; 265. Specification NF-ISO 6743 classified DAJ areas for heavy |